## Slide 1: Safety design parameters for Li-ion propulsion batteries and interaction with vehicle manufacturers to achieve EV safety
Electric Vehicle Safety Technical Symposium
NHTSA
May 18, 2012
Mohamed Alamgir
LG Chem Power

## Slide 2: Introduction
Battery safety involves interactions from cell component to the battery system level.
It might not be a stretch to state that seemingly unsafe cell system can be made safe by the use of a design or operating parameters that can ensure highly reliable and safe operation.
The converse can also be true. An apparently robust cell system can fail due to the improper choice of module/pack system parameters.
Hence, cell/battery manufacturers and vehicle OEMs work very closely together to ensure the development/deployment of safe battery system.

## Slide 3: Battery Safety Design Considerations
Battery safety is achieved through layers of protection:
  Individual cells
  Groups of cells (modules)
  Pack
    Structure and internal assemblies
    Thermal Management
    High Voltage circuits
    Battery Management & Control

## Slide 4: Battery Safety Design Considerations
Interactions within the battery system (especially under abuse/abnormal conditions) can be complex, but are managed using advanced engineering tools
  Design Failure Mode and Effects Analyses
  Failure Tree Analyses
  Test to failure
  Abuse testing
Failures in one or more components within a pack can be isolated or contained to prevent cascading of failures.

## Slide 5: Safety Parameters: Cell Level
Utmost attention is paid toward designing a cell that is safe.
In fact, we can easily say that mechanical, thermal and electrical safety considerations dictate the selection of all cell components!
Requirements
  Highest Thermal Stability
  Large Voltage Stability Window
Key Cell Components
Cathode
Separator
Electrolyte
Case design
      Metal case
      Laminated packaging

## Slide 6: Cell Safety: Cathode Selection
Several cathodes are now in use in large-format batteries.
  Spinel (LiMn2O4)
  NMC (LiNiMnCoO2)
  NCA (LiNiCoAlO2)
  LFP (LiFePO4).
For design purposes, balance is sought among safety, power, energy, life and cost.

## Slide 7: Cell Safety: Anode; Electrolyte
Current anodes overwhelmingly are carbon based. There are subtle differences in their abuse-tolerance behavior depending on, among others, their surface area, etc. However, their overall response under abuse-condition is quite similar.
Current electrolytes are all based primarily on organic carbonate solvents. Stability at the anode as well as at the cathode are considerations that play a key role in selecting the electrolyte system.

## Slide 8: Cell Safety: Separator
Separators not only have the role of keeping the anode and cathode apart from each other, they also need to be very robust with respect to mechanical/thermal stress in course of life.
With this goal in mind, separators have been developed which are mechanically much more robust than their conventional counterparts.
These separators have low shrinkage at elevated temperatures and are resistant to internal shorts.

## Slide 9: Cell Safety: Cell Case
Metal Can: Usually equipped with safety devices such as a safety-vents which become activated when certain amount of pressure is generated within the cells.
Laminated Packaging: Quite a few manufacturers prefer the laminated packaging (or pouch) for a number of reasons, such as ease of manufacturing, lower cost, easier scale-up and most importantly
  The pouch design allows the release of gas at high pressure and temperature without the building-up to an unsafe level.

## Slide 10: Cell Safety: DFMEA
Rigorous DFMEA is carried out for cells under operating and abuse conditions. For example,
      This involves mechanical dimensions of electrodes, separators.
      Cathode to anode ratios, electrolyte amounts, etc…..
Abuse- Conditions
      Thorough analysis is carried out to identify design parameters that could result in unsafe operating conditions.
Extensive Review with OEMs.

## Slide 11: Cell Safety: Abuse- Testing
Comprehensive testing is carried out to characterize and identify range of voltage, temperature, mechanical deformation etc. that might lead to unsafe battery conditions.
Not only are USABC, SAE –standard tests are carried out, additional tests outside of these tests requested by the OEMs are also carried out.
These tests are further augmented by UNDOT tests to simulate shipping conditions.

## Slide 12: Cell Safety: Examples of USABC Abuse- Testing
Test Item | Conditions
Nail Penetration | 3 mm sharp nail SOC 100% 55 oC
Cell Crush | 80 mm/min 50% crush SOC 100% 55oC
Overcharge | 32A 6.3V 55oC
Overdischarge | 1C rate discharge from SOC 100% to SOC 100% for 2 hrs 55˚C
External Short Circuit | 5 mΩ SOC 100% 55oC

## Slide 13: Module/Pack: Design for Safety
Modules/packs are built with the utmost attention for the physical/thermal/electrical protection of the cells to ensure safe operation as well as performance and life during the life of the vehicle.
Cell/battery manufacturers work very closely with the OEMs to ensure that the battery is provided the best location from safety point of view.
They are subjected to a wide array of mechanical, electrical and environmental validation tests developed in close cooperation with the OEMS.

## Slide 14: Module/Pack: Design for Safety
Built to attain complete electrical isolation of the battery pack from the vehicle. An HVIL (High Voltage Interlock System) is used to prevent exposure of occupants to high voltages.
High- voltage and low-voltage lines are separated for electrical safety.
High-voltage (busbars, contactors, connectors) circuits are made in such a way that they survive stress/abuse during vehicle life.
BMS (battery management system) carries out critical safety functions such as charging and health management
    Opens the contactors when voltage, current and temperature limits critical from safety points of view are violated.

## Slide 15: In conclusion……
While battery safety is better understood within the context of an overall battery system, focus of all cell design and development work is the manufacturing of abuse-tolerant cells and hence tremendous effort is devoted toward selecting cell materials that are safe.
Cell/battery manufacturers and vehicle OEMs work in close cooperation with each other to develop abuse-tolerant cells and packs.
Extensive validation tests in conjunction with the OEMs using industry-standard procedures to identify parameters that are critical for the safety of Li ion propulsion batteries.